Flexible, Thick Glue Lined Dual Wall Heat Shrinkable Tube G-3X-T

Application:

Flexible, Dual Wall Heat Shrinkable Tube Thick Adhesive is manufactured by co-extrusion of polyolefin and hot-melt adhesive. Designed to provide both insulation and sealing for protected articles. Used to protect bundles wires and metal tubes against water and moisture.

Features:

1.         Flexible, thick adhesive lined to bond to a wide variety of plastics, rubber and metals

2.         Operating Temperature: -45℃～125℃

3.         Shrinking Temperature: Start at 70℃, and shrunk totally at 125℃

4.         Shrink Ratio: 3:1

| Dimension |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Size |  |  | As Supplied | After Recovery (mm) |  |  |  |  |  | Standard package(m/spool) |
|  |  |  | Inner diameter |  |  |  |  |  |  |  |
| mm | Inch |  | Internal Diameter(mm) | Total wall thickness |  | Wall thickness ofadhesive layer |  | Inner diameter |  |  |
| 3.2 | 1/8 |  | 3.2 | 0.95±0.15 |  | 0.45±0.10 |  | 1 |  | 200 |
| 4.8 | 3/16 |  | 4.8 | 1.20±0.15 |  | 0.60±0.10 |  | 1.6 |  | 100 |
| 6.4 | 1/4 |  | 6.4 | 1.35±0.15 |  | 0.70±0.10 |  | 2.2 |  | 100 |
| 7.9 | 5/16 |  | 7.9 | 1.50±0.15 |  | 0.75±0.10 |  | 2.7 |  | 100 |
| 9.5 | 3/8 |  | 9.5 | 1.65±0.15 |  | 0.85±0.10 |  | 3.2 |  | 50 |
| 12.7 | 1/2 |  | 12.7 | 1.80±0.20 |  | 0.90±0.10 |  | 4.2 |  | 1m/pc |
| 15 | 5/8 |  | 15 | 1.80±0.20 |  | 0.90±0.10 |  | 5.2 |  | 1m/pc |
| 19.1 | 3/4 |  | 19.1 | 2.00±0.20 |  | 1.00±0.10 |  | 6.3 |  | 1m/pc |
| 25.4 | 1 |  | 25.4 | 2.10±0.20 |  | 1.05±0.10 |  | 8.5 |  | 1m/pc |
| 30 | 5/4 |  | 30 | 2.20±0.20 |  | 1.05±0.10 |  | 10.2 |  | 1m/pc |
| 38.1 | 1 1/2 |  | 38.1 | 2.40±0.20 |  | 1.15±0.10 |  | 13.5 |  | 1m/pc |
| Technical Data |  |  |  |  |  |  |  |  |  |  |
| Property |  |  | Test Method |  | Test Result |  |
| Tensile Strength, MPa |  |  | ASTM D2671 |  | ≥10.4 |  |
| Elongation, % |  |  | ASTM D2671 |  | ≥300 |  |
| Tensile Strength after aging, MPa |  |  | UL 224, 158℃X168h |  | ≥7.3 |  |
| Elongation after aging, % |  |  | UL 224, 158℃X168h |  | ≥20 |  |
| Dielectric strength(kV/mm) |  |  | IEC 243 |  | ≥15 |  |
| Volume resistance Ω.cm |  |  | IEC 93 |  | ≥1X1014 |  |
| Hot melt adhesive |  |  |  |  |  |  |
| Property |  |  | Test method |  | Test Result |  |
| Water absorption |  |  | ASTM D570 |  | ≦0.2% |  |
| Softening point |  |  | ASTM E28 |  | 95℃ |  |
| Peel strength(PE) |  |  | ASTM 1000 |  | 120N/25mm |  |
| Peel strength(PA) |  |  | ASTM 1000 |  | 80N/25mm |  |